### S-Q-55-03			14/08/2003				P. 1/2

# P P I  REFLECTIVE  COATING

## PRODUCT  DESCRIPTION  :

This product is intended as a specialty coating for marking surfaces where night  reflectivity is required.  P P I  Reflective Coating provides more vertical reflective  marking for steel, aluminum, concrete, and wood substrates than normal traffic  paint can do.  This product dries to a finish that reflects light back at the source.

P P I  Reflective Coating is more visible compare to any other traffic marking  material especially at night time and during dark rainy conditions

SURFACE  PREPARATION  :

Surfaces to be painted should be cleaned and freed from any soil or oil compounds.

For best results, the surface should be lightly abraded before coating.  For metal  surfaces, areas that show corrosion or bare metal should be abraded to remove the  corrosion then it should be coated with metal primer, allow the primer to dry completely before application of PPI Reflective Coating. The Reflectivity and durability of this material is totally relevant to the surface preparation, it is therefore advised to observe the correct and proper surface preparation and application of this material.

APPLICATION  :

Mix P P I  Reflective Coating on a paint shaker before application.  Proper mixing is very important to achieve optimum reflective properties. Alert can be applied by spraying, brushing, stenciling, or rolling.  Best properties can be obtained by spraying with a tip size of 0.015 in with 10-20 psi.  Apply in wet uniform coats until substrate is appropriate color.  Extremely wet coats will not reflect as well as

a drier coat.  When rolling Alert, use a foam roller while rolling in one direction only.  Do not apply Alert over latex coating or below 55 F.  Odorless Mineral Spirits may be used as a reducer and for clean up.

### S-Q-55-03			14/08/2003				P. 2/2

PHYSICAL  PROPERTIES  :

Appearance  :					Bright White

Weight per container  :				1 kg.

Fineness of Grind  :				200 mesh

Gloss  :						5 max @ 60

Solids by Weight  :				85.0 %

by Volume  :				58.4 %

Volatile Organic Content  :			2.85 lbs./gal. or 342 g/L

Coverage  :						937 sq. ft./gal. @ 1 mil DFT  or

10-15 sq.m/L  @ 51-80 m (2-3 mil)

Dry Time @ 1 mil DFT  :			Tack Free  :     1-2 hours

Dry Hard   :     24 hours

Durability	Equivalent to oil-based paint on a similarly applied surface ( more than 1 year depending on the surface preparation and application ).

Reflectivity                                                     6 to 8 months, then the surface must be recoated to maintain reflectivity good as new.

PRECAUTIONS  :

Use with adequate ventilation and proper safety equipment.  See MSDS for complete details of composition and required precautions for safe use.

Because  we  cannot  anticipate  or  control   the  many  different  conditions under  which  this  information  and  our  products  may  be  used,  we  do  not  guarantee  the  applicability  or  the  accuracy  of  this  information  of  the  suitability  of  our  products  in  and  given  situation.  Users  of  our  products  should  make  their  own  tests  to  deforming  the  suitability  of  each  such  product  for  their  particular  purposes. The  products  discussed  are  sold  without  such  warranty,  either express  or  implied.  Also,  statement  concerning  the  possible  use  of  our products  are  not  intended  as  recommendations  to  use  our  products  in  the  infringement  of  any  patent.  All  chemicals  may  present  unknown  health  hazards  and  should  be  used  with  caution.  Although   certain  hazards  are  described  in  this  publication,  we  cannot  guarantee  that  these  are  the  only  hazards  which  exist.  Users  of  any  chemical  should  satisfy  themselves  by  independent  investigation  of  current  scientific  and  medical  knowledge  that  the  material  can  be  used  safely.